Proceedings of the International Laser Technology Congress AKL´10

Finalists of the Innovation Award Laser Technology 2010

New repair technique for aero-engine components using 
Laser Metal Deposition

Dipl.-Ing. Jürgen Dupré

Team Representative:

Dipl.-Ing. Jürgen Dupré

Repair Engineering Specialist, IPT Lead
Rolls-Royce Deutschland Ltd. & Co. KG

Dahlewitz

Members of the project management team:

Dipl.-Ing. Jürgen Dupré, Repair Engineering Specialist, IPT Lead
    Rolls-Royce Deutschland Ltd. & Co. KG, Dahlewitz

Certified Engineer Elke Weiss, Repair Engineer
    Rolls-Royce Deutschland Ltd. & Co. KG, Oberursel

Dipl.-Ing. Gerhard Backes, Project Leader Repair Processes
    Lehrstuhl für Lasertechnik LLT, RWTH Aachen University

Dr. Andres Gasser, Group Leader Laser Metal Deposition
    Fraunhofer-Institut für Lasertechnik ILT, Aachen

Areas of application

- Gas turbine repair and overhaul

- Aero engine repair and overhaul

- Stationary turbines (power generation) repair and overhaul

- Gas turbine production

Technological impact

- New repair process for aero-engine components

- Reduced process costs

- Shorter development lead time

- Improved quality assurance

Abstract

With an increasing number of engines being operated under “Flight Hour Agreement”

terms, Rolls-Royce has to find ways to minimise the operating costs of hardware.

Therefore innovative repairs of key components are vital to achieve that goal. One

innovative approach to this is Laser Metal Deposition, which enables the restoration of

features that were previously classified as non repairable.

Processes like Direct Metal Deposition (DMD) and adaptive machining are being

developed to accommodate such challenges by repairing instead of replacing. With a

focus on high value / high volume parts made of Titanium or Nickel material (e.g. Blisks,

HPC-Drums, Casings, HPT-Discs), Laser Metal Deposition is gaining more and more importance. This enables successful repair of components returning from service as well

as the salvage of parts damaged during new part manufacture, which previously was not

feasible.

Laser Metal Deposition (LMD) works usually with a powder, which is fed into the interaction area between the laser and the component. The laser melts a small portion of the base material and the powder leading to a metallurgical bonded layer. The heat input is extremely low due to the fact that the laser can be focused to small areas and does only interact at this particular area means there is no interaction with closely surrounding features. Also the laser power can be adjusted with high precision, thus avoiding distortion of the component and micro structural changes. Key to the process is the development of new powder feeding nozzles as well as the development of repair procedures that are capable of applying a local shielding atmosphere during the repair process, without having to place the components in a process chamber.

The BR700-715 HP Compressor Front Rotor Drum Assembly is, for example, a rotating titanium component. In service wear caused by the damping wire as well as the retaining groove lock plate leads to a component that must be declared unserviceable. The damage is beyond acceptance limits and also beyond limits to allow repair using alternative techniques such as thermal spray or TIG welding. The capability to return a high value rotating titanium component previously thought not to be repairable, within a relatively short development time frame, is an innovative technical improvement for the repair capabilities within Rolls-Royce.

1. High value components suitable for the repair with Laser Metal Deposition

(Photo: Rolls-Royce Deutschland Ltd. & Co. KG)

2. Laser Metal Deposition process for the repair of the retaining grove lock plate of an HPC front drum

(Photo: Fraunhofer-Institut für Lasertechnik ILT, Aachen, Germany)